Polyester Filter Cloth

There are 3 series of polyester/ PE filter cloth

- PET multifilament (long thread) filter cloth

- PET monofilament filter cloth

- PET multifilament / monofilament filter cloth

Applications

Dedusting, separation in solid and liquid filtration, for filter press, conveyor belts filtration, vacuum filter, chemical industry, food and beverage industry, metallurgy, building section and miming industry and etc.

Representative products

Normal filter cloth  747 , 758, 729 , 208 . 130 , 240 , 260

Thicker and with higher density 3927 , 4030, 822, 621

Crossing weave filter cloth  903 , 3751 , 3850

Blow is the list of PET filter cloth we providing

Model     Breaking strength   Density     Thickness  Weight   Air Permeability  Weave

(N/5*20CM)      (root/10cm)   (mm)      (g/m2)     (L.m2.s)

60-8(130)     1363/111.3     260/221.6     0.27      125.6    130.6       Plain

60-10(240)    2508/958      225.6/156     0.42      219.47    36.1       Plain

60-9(260)     2202/1776     205.6/160.8    0.47      257      32.4       Plain

60-7(621)     3026/2288     191.2/134     0.65      342.4     37.8       Plain

5926(120-7)   4498/4044     260/202      1.42      610       54        Twill

734(120-12)   2072/1633     232/166      0.62      245       480       Twill

745(120-13)   1936/730      232/196      0.48      210       125       Plain

747(120-14)   2026/1485     226/158      0.53      248       120       Plain

758(120-15)   2594/1909     194/134      0.73      330       100       Plain

3927(120-16)  4598/3154     156/106      0.9       524       18        Plain

728(120-17)   2753/1869     246/310      0.89      360       180       Twill

729          3180/2157     307/201      0.72      315       120       Satin

208          2788/1930     360/276      1.43      400       280       Twill

822          5760/3480     260/102      1.65      940       22        Twill

We are able to manufacture up to your order! Plain, till and satin weave are available on your request or as your sample.

Polypropylene filter cloth

There are 3 series of polypropylene/PP filter cloth

1.PP multifilament (long thread) filter cloth

2.PP monofilament filter cloth

3.PP multifilament / monofilament filter cloth

Applications

Separation in solid and equip with filter press, conveyor belts filtration Machine, filter leaf, horizontal rotating pan filter, vacuum filter, in chemical industry , fertilizer industry, sugar making, food and beverage, metallurgy, building, waster water dealing, and so on.

Representative products

Thinner filter cloth  521, 522, 4212, 750A

Thicker and with higher density  750B(series),750AB, 2402, 5422, 5514, 6320, 7640

Below is the list of PP filter cloth we providing

Model     Breaking strength   Density     Thickness  Weight   Air Permeability  Weave

(N/5*20CM)      (root/10cm)   (mm)      (g/m2)     (L.m2.s)

521        2608/2050       214.8/150.8    0.79      302.7       216.5      Twill

522        2104/1633       244/173       0.41      155        73.44       Plain

534        2501/1894       193.6/100      0.99      368.1      41.2        Plain

4212       2672/1342        236.4/123.2   1.34      389.4      85.6        Twill

700A       3426.6/2819.4     204/1006     0.7       350       117.9       Plain

700B       4648/2866.6      188/114       0.59      280       254.2       Twill

700AB      6865.4/416.7      378/235      1.15      580       82      Twill+Plain

750A(840A)   4466/2905      168/131       0.86      330      42          Plain

750B(840B)   5234/3489      256/141       0.99      420      76         Twill

750AB(840AB) 6718/5412      333.8/204.4   1.36      489.9     24.5        Plain

840-1         5275/3948      525/146      0.9       440      45.5        Twill

840-2         5928/4086      383/142      1        490      40.7        Twill

830-3         6282/4858      311/134      1.1       520      27.2        Twill

858           4418/3618      251/124      0.88      380     340.7       Twill

4218          8568/5427      456/94       1.32      660     38.4        Twill

4422          2643/1514      181/94       1.18      480     17.86       Twill

1000A        5585/4089.2     204/102      0.85      435     9.83        Plain

1000B        6636/1481       204/110     0.79       430    21.49        Twill

1500-1        5628/3701      251/118      1.42       725    29.8        Twill

108B         8721/4642       503/133     1.1        600    13.6       Double Twill

108C         8367/4797       504/177     1.03       600    22.96       Satin

Monofilament filter cloth

The Mono filament fabrics including 4 series

PET monofilament filter cloth

PP monofilament filter cloth

PA  monofilament filter cloth

PVC monofilament filter cloth

Properties of monofilament filter cloth

The surface finishing of Pyrocondensation and canlandered will make filter cloth reach highest filtration efficiency , good cake discharge, good cake washing, highest tensile strength, longer using life.

Main Applications

Separation in solid and liquid to equip with filter press, conveyer belts filtration machine, rotary disc, rotary drum , in chemical industry, miming industry, coal industry, food and beverage, metal smelting, waste water dealing, and so on.

Below is the list of Mono filament fabrics we providing

Model      Density         Thickness      Weight      Air Permeability

(root/10cm)      (mm)          (g/m2)     (L.m2.s)

903         286/202         0.73          320        135

3013        300/150         0.75          580        less than 4.0

3751         145/100        1.04          758        less that 4.0

3950         152/98         1.14          786        less that 4.0

9898         228/149        1             1080       less that 4.0

FL928        290/250        0.74          326        126

PA2304       600/240        0.42          310        780

PA2319       492/228        0.64          370        608

PA2320       600/240        0.42          310        780

PA2322       492/228        0.64          370        608

PA5916       504/160        0.48          355        200

PP2448       310/134        0.98          600        18

PP2471       472/158        0.95          525        15

PP2812       284/118        0.88          285        4115

PP3127       540/228        0.42          250        730

PP3130       480/216        0.42          245        680

PP3135       1050/440       0.31          310        420

PP5422       535/220        0.97          570        25.5

PP5514       620/142        0.76          405        360

PP5722       1140/456       0.48          268        210

PP6022       630/216        0.65          325        105

PP7024       140/456        0.48          268        210

PP7242       284/165        0.48          820        /

PP7640       285/165        1.55          850        2.5

Polyamide Fabrics

There are 3 series of Polyamide/PA filter cloth

- PA multifilament (long thread) filter cloth

- PA monofilament filter cloth

- PA multifilament / monofilament filter cloth

Main Applications

Separation in solid and liquid to equip with filter press, conveyor belts filtration machine, filter leaf, horizontal rotating pan filter, vacuum filter , in chemical industry , mining industry, coal industry, building, waste water dealing, and so on.

Below is the list of PA filter cloth we providing

Model     Breaking strength   Density     Thickness  Weight   Air Permeability  Weave

(N/5*20CM)      (root/10cm)   (mm)      (g/m2)     (L.m2.s)

107       1913/1539         240.8/187.2   0.42       195.4      29.7         Plain

633       2390/2202         236/156      0.58       300        23          Plain

601       3410.75/3365       132.0/160.8   0.49       315        125         Plain

301       2016/1981         275.0/250.0    0.22       106.8       114.4       Plain

Polyvinyl alcohol staple fabric

There are 3 series of Polyvinyl/ PVA filter cloth

295-1A  Good heat absorption, Mainly used in rubber industry.

385-102  High breaking strength , good anti attrition. Mainly used in high-pressure press filter.

295-104  Low breaking strength , good air permeability, mainly used in low-pressure press filter and rubber finished product of low strength.

295-1: strong breaking strength. Mainly used in plate ad frame press filter.

Below is the list of PVA filter cloth we providing

Model     Breaking strength   Density     Thickness  Weight   Air Permeability  Weave

(N/5*20CM)      (root/10cm)   (mm)      (g/m2)     (L.m2.s)

295-A      4302.2/2138.4     100.0/64.6    1.56       555.8     43.7          Plain

295-102     1706/1556       188/141      0.71       360       29           Plain

295-104     1591/1141       232.1/164     0.58       246.9     40.5          Plain

295-1       2410/2630       157/110       0.95      50.8       15           Plain